- A Critical review of parameters optimization for Electron beam Welding

Abstract:

This review paper unequivocally highlights the essential role of machine learning models in enhancing weld quality and optimizing welding processes, with a strong focus on the revolutionary applications of ML in electron beam welding. By adopting these innovations, the industry can confidently unlock new levels of efficiency and excellence in welding technology. The formation of brittle Ti–Fe intermetallic compounds (IMCs) and the mismatch in thermal properties make welding titanium and stainless steel difficult. These dissimilar metals can be joined using Electron Beam Welding (EBW), which is done under high vacuum and provides precise control with little contamination. The viability of employing various filler and interlayer materials, including graded stacks and Nb, Ta, V, Mo, Cu, and Ni, is investigated. The study assesses how well they work to strengthen joints, lower IMCs, and increase corrosion resistance. While Ni may encourage brittle phases, refractory metals like Nb and Ta are predicted to yield the best results. The result will assist in determining workable welding parameters and filler materials. The formation of brittle Ti–Fe intermetallic compounds (IMCs) and the mismatch in thermal properties make welding titanium and stainless steel difficult. The viability of employing various filler and interlayer materials, including graded stacks and Nb, Ta, V, Mo, Cu, and Ni, is investigated.. Finding workable filler materials and welding parameters for dependable Ti–SS joints will be made easier by the results. Furthermore, the study offers a comparative framework that can be used as a guide by businesses looking for dissimilar metal joints in advanced engineering applications that are lightweight, corrosion-resistant, and mechanically dependable

Keywords: LBM, machine learning, performance, efficiency, material characterization, filler material selection, and weldability testing.

Diffusion barrier, beam offset, heat input, microstructure, mechanical properties, residual stress, titanium, Ti-6Al-4V, commercially pure titanium, stainless steel, 304L, 316L, 410/420, intermetallics, interlayer, filler, copper, nickel, vanadium, niobium, tantalum, molybdenum, and feasibility

1. Introduction:

Electron beam machining (EBM) is a crucial technique in non-conventional manufacturing and precision engineering. This technology utilizes a focused beam of electrons to perform a range of material processing operations. EBM utilizes a high-energy electron beam to remove or modify layers of material on the surface of a workpiece.  That is achieved through processes such as ablation, vaporization, or melting. LBM leverages the unique properties of electron light, including its coherence, monochromaticity, and high intensity, to remove material with remarkable precision and control.

Electron Beam Welding

Microoperations excel in precision engineering, enabling the accurate drilling of tiny holes, the meticulous carving of intricate designs, the detailed engraving of markings, and the sophisticated sculpting of complex curves. This technique is versatile and can be applied to a diverse range of materials, including metals, polymers, ceramics, and composites, making it an essential tool in advanced manufacturing and craftsmanship.

Electron beam machining (EBM) represents a groundbreaking advancement in manufacturing technology. It provides a non-contact process that greatly reduces thermal distortion and damage. By entirely eliminating the risks of tool wear and damage commonly associated with traditional machining methods, EBM not only enhances operational efficiency but also achieves exceptional precision. This state-of-the-art technique is reshaping industries and establishing new benchmarks for quality and reliability in machining processes.

The extensive applicability of EBM across various sectors highlights its significant influence. Industries such as aerospace, automotive, electronics, and medical device manufacturing are leveraging the advantages of EBM to drive innovation and excellence.

In the aerospace sector, Electron Beam Melting (EBM) is a crucial technology for manufacturing lightweight components with intricate geometries. This advanced production process not only enhances design

flexibility but also lessens heat-affected areas during production, protecting the components' performance and structural integrity. Engineers can create parts that are not only reliable and efficient but also specially designed to satisfy the demanding specifications of contemporary aerospace applications by employing EBM. This ability is critical to guaranteeing the longevity of critical parts. In the medical industry, Laser Beam Melting (LBM) makes it easier to precisely fabricate intricate medical devices and implants while guaranteeing patient safety and biocompatibility.

Titanium and stainless steel are extensively utilized in industries such as aerospace, nuclear, chemical processing, and biomedical engineering due to their exceptional mechanical properties and resistance to corrosion. However, titanium and stainless steel cannot be directly joined because of their chemical incompatibility. As a result, brittle Ti–Fe intermetallics (TiFe, TiFe₂) are formed, which drastically lower joint ductility and toughness. Moreover, differences in melting points and thermal expansion coefficients increase residual stresses and distortion.

Electron Beam Welding (EBW), a high-tech fusion welding process that creates deep penetration and high energy density under high vacuum, uses a concentrated electron beam. Among its advantages are precise heat input control, low contamination, and small heat-affected areas. These features make EBW a promising method for welding titanium to stainless steel when combined with the appropriate filler or interlayer materials. Interlayers like Nb, Ta, V, and Mo function as diffusion barriers to suppress Ti–Fe intermetallics, while Cu can act as a buffer and graded stacks can further tailor the transition between the two metals. In order to create mechanically reliable, sound, and defect-free Ti–SS joints, this study aims to ascertain whether EBW with different interlayer combinations is practical.

1.1 Literature Review:

Ahmad Naseem et al. [2] conducted experimental research on electron beam welding of low-nickel nitrogen-stretched austenitic stainless steel to investigate its mechanical properties. They found a 90% improvement in strength compared to the base alloy, while microhardness decreased by 12.9%. Additionally, they noted that the impact energy was reduced by 50% when compared to the base material.

Dutilleul T et al. [3] also explored electron beam welding, focusing on its application in high-productivity welding of thick-section components within the nuclear industry. Their research highlighted the use of small modular reactors for joining thick-section pressure vessel components. They identified the operation of the Pro-Beam K 2000 system within a chamber for electron beam applications at the Nuclear Advanced Manufacturing Research Centre.

Min Cheng et al. [4] conducted an experimental study on electron beam welding, focusing on the joining of a novel high-temperature titanium alloy powder compact. They also investigated the effects of annealing treatments on the microstructure and mechanical properties of the EBW joints.

Meanwhile, Konrad Kerber et al. [5] explored the critical welding speeds that distinguish between conduction (at low welding speeds) and non-conduction (at higher welding speeds). Their study utilized various methods, including light optical microscopy, electron backscatter diffraction measurement, ultrasonic testing, in situ thermal imaging, electrical resistance measurement, and tensile tests. The joints achieved up to 98% of the specific electrical conductivity of the international annealed copper standard.

Zbigniew Wencel et al. [6] conducted an experimental study on the welding process by exploring two values of electron beam de-bunching, each with different widths, while taking into account various welding parameters. The subsequent heat treatment involved tempering at 520°C for 3 hours, followed by a single freezing process at -84°C for 3 hours, in combination with another single temperature treatment at 520°C for 3 hours.

Bauer A. et al. [7] also carried out experimental studies, demonstrating that tailored processing parameters—such as pre-heating with an electron beam or beam oscillation during welding—facilitated defect-free joining with very thin weld seams and a minimized heat-affected zone. Nonetheless, despite the choice of welding parameters, some specimens exhibited the formation of smaller grains within the former fusion zone.

Marta Lipinska et al. [8] conducted experimental studies aimed at reducing energy input during welding, which in turn minimizes the heat-affected zone and limits the evaporation of elements with high saturated vapor pressure. The weld efficiency for the CG alloy was found to be 80%, whereas for the UPG sample it was 68%, representing 82% of the efficiency compared to the CG base material.

Vadim S. Tynchenko et al. [9] developed a mathematical model that employs machine learning techniques to predict effective process parameters. This research utilized regression analysis algorithms, such as ridge regression and the random forest regressor, as predicting process parameters necessitates a regression model. All models successfully addressed the task, achieving a forecasting accuracy of at least 89%. The weld depth exhibited a second-degree polynomial relationship with a regularization of 10^-5, while the weld width demonstrated a third-degree polynomial dependence with a regularization of 10^-4.

Jia Tao et al. [10] conducted an experimental study comparing FEM simulations using a 2D Gaussian heat source. They performed an EBW experiment on niobium sheets to validate the simulation results. The mechanical findings indicate that the peak longitudinal stress in the weld center, the peak transverse stress in the weld center, longitudinal distortion, and transverse distortion predicted by the designed model deviate from the experimental results by only -4.88%, -4.03%, -9.32%, and -5.98%, respectively.

In the study by Tynchenko V.S. et al. [11], various algorithms suitable for addressing the regression problem are examined. The implementation of these algorithms is expected to enhance the quality of the regression model. Additionally, utilizing assessment methods and forecasting techniques will help decrease the time and labor required for searching, developing, and refining the process. This proposed approach aims to assist specialists in electron beam welding in making informed technological decisions during the development of technological processes and when introducing new product types into production.

Ariel Rokem et al. [12] examined one of the challenges of using ridge regression: the necessity to set a hyperparameter (alpha) that controls the level of regularization. This process can become cumbersome when analyzing large datasets. The current work addresses these issues through an innovative approach to ridge regression. We present an algorithm that efficiently implements this approach, referred to as fractional ridge regression, along with open-source software implementations in both Python and MATLAB (https://github.com/nrdg/fracridge).

Vasundhara Singh et al. [13] conducted an experimental study by manipulating the magnetic lens aligned with the electron beam to investigate the diameter of the oscillating beam (OD) and its impact on weld quality. The OD was varied between 0.5 mm and 2 mm. A comprehensive array of tests, including X-ray diffraction, scanning electron microscopy (SEM), electron backscattered diffraction, as well as assessments of hardness, wear, and tensile properties, were employed to characterize the weld quality. While the weld strength was found to be lower than that of the base metal, the introduction of BO improved the welds' ductility and strength.

Zagornikov V.I. et al. [14] examined the necessity of repairing the cathode unit, prompted by instances of imported insulators displaying defects, specifically a thickness deviation of 0.5 to 1.0 mm in the metal flange at the brazed joint with the insulator. It was essential to address the repercussions of improper mechanical treatment of the insulator collar following brazing. The repair technologies utilized circumferential insert bandages of varying configurations for two scenarios, aimed at rectifying welding defects related to both localized repairs of the edge and the repair of more extensive areas.

Jozef Beata et al. [15] conducted an experimental study on the thickness of 25.4 mm for AW 2099-T83 aluminum lithium alloy, utilizing electron beam welding with an accelerating voltage of 55 kV to produce welded joints. The welded joints underwent inspection through computed tomography, macroscopic and microscopic analysis, tensile strength tests, and microhardness measurements. The fracture occurred in the weld metal during the tensile strength testing.

Mohamed .M Jameel et al. [16] conducted an experimental investigation into the electron beam welding process, where a high-speed stream of electrons is precisely focused on the weld spot. This method is widely utilized in the aerospace and defense industries due to the narrow fusion zone it creates, resulting in less metal being melted during the joining process. Consequently, this leads to reduced distortion and minimized heat impact. The electron beam welding process is inherently complex and is influenced by a variety of parameters. The input parameters for welding are crucial in determining the quality of the weld, and they include factors such as accelerating voltage, beam current, depth of penetration, beam focal diameter, and welding speed.

Oleksii Fedosov et al. [17] conducted experiments demonstrating that electron beam welding can effectively join 40 mm thick VT23 and VT3-1 titanium alloys, overcoming the challenges associated with deep penetration in conventional welding methods. To achieve high strength (exceeding 1250 MPa) and impact toughness (48-50 J/cm²) in these titanium alloys following the electron beam welding process, post-weld heat treatment is crucial. Additionally, advancements in welding modeling have enhanced reproducibility, quality, and efficiency, resulting in welded joints that possess properties comparable to those of the base metal.

Rai et al. [18] conducted an experimental study on three-dimensional heat transfer and fluid flow during keyhole electron beam welding, taking into account the variable temperature of the keyhole walls. The model they developed was applied to 304L stainless steel welds created with different power density distributions, which were achieved by varying the focal spot radius while maintaining a fixed input power. Their findings highlight the significance of convective heat transfer in the weld pool during the electron beam welding process.

Zenin A.A. et al. [19] conducted an experimental study on the effects of temperature on the structure of brazed titanium-alumina joints. Their research utilized electron beam brazing in conjunction with a plasma-cathode source. They found that brazing below the titanium alpha-beta transition temperature enhances joint performance. As a result of these studies, a robust and tight metal-ceramic joint between titanium and alumina ceramic was successfully achieved.

Nesterenkov V.M. et al. [20] also conducted experiments at the Paton Electric Welding Institute, which focuses on advancing technology and equipment for electron beam welding, surfacing, and prototyping, particularly for modern structural alloys. The equipment developed is employed for joining complex structures across various industries, as well as for the restoration and repair of components, such as parts used in gas turbine engines.

Shapovalov et al. [21] conducted an experimental investigation into the mechanical properties of steels subjected to highly concentrated energy sources, such as plasma. There is a notable scarcity of research addressing the role of nitrogen in metal melts within the plasma-slag process. At partial nitrogen pressures below 0.1 atm above the melt, temperatures ranging from 1823 to 2323 K have minimal impact on the nitrogen content in steel. Conversely, at higher partial pressures, the nitrogen content in steel tends to decrease as the temperature rises. Under the experimental conditions, the melt temperature was evaluated to be 2385 K. It was found that the nitrogen distribution coefficient between the metal and slag remains relatively stable, measuring between 1.1 and 1.2 at partial nitrogen pressures up to 1 atm.

Skryabinsky et al. [22] conducted experimental studies on the mechanical properties of joints and the distribution of hardness in the heat-affected zone (HAZ) of 2219 alloy plates. These plates were quenched prior to welding and subjected to artificial aging afterward. They observed an improvement in the ultimate strength of the joints, increasing from 300-315 MPa to 385-395 MPa, along with a rise in hardness of both the weld and HAZ metal by 5-10 HRB. Through measuring the thermal cycles of the welding process, it was found that the maximum heating temperature in this region reached approximately 590°C. At a welding speed of 20 mm/s, a decrease in metal hardness by 2-3 HRB was noted, with an HAZ width of about 8 mm.

Akhonin et al. [23] performed experimental studies on the melting of low-grade nickel scrap to produce semi-finished products, which include hot- and cold-formed seamless pipes, capillarity pipes, and thin- and thick-walled pipe variants, as well as rings, squares, and hexagons. To assess quality, comprehensive research was conducted on the manufacturing of semi-finished products in the form of elongated soft rods with a diameter of 40 mm and wire with a diameter of 3 mm. The study determined that the mechanical properties of the semi-finished products from EBM nickel fully comply with standard requirements.

Radoslav Vandzura et al. [24] conducted an experimental study on electron beam welding in collaboration with First Welding Company Inc. The objective of this experiment was to create a weld joint between aluminum alloys prepared using additive and conventional methods. They aimed to evaluate the base materials, the heat-affected zone, and the weld joint in terms of microstructure, as well as to measure and assess microhardness.

Maksymov S.Yu et al. [25] experimentally investigated the cooling rates of different areas of weld metal in both wet underwater welding and welding in air. They determined how the volumetric fractions of phase components such as ferrite, austenite, and excess phases changed in the microstructure of the heat-affected zone (HAZ) metal as a function of cooling rate. The phase transformations primarily occurred in the high-temperature heat-affected zone within the temperature range of T = 1300-800°C, while the contribution of the low-temperature heat-affected zone (T = 800-500°C) to changes in phase components was found to be negligible.

Korotynskyi O.Ye et al. [26] conducted an experimental study on pulsed welding currents of regulated shape. The necessity for such currents arises primarily from the objectives of pulsed technologies, where the shape of the load currents ensures the required timing of power input into the technological object. Notable applications of these technologies include pulsed laser welding, laser heat hardening, and laser piercing, among others. Special pulsed current generators are needed to create such energy profiles.

Sihui Yang et al. [27] conducted an experimental study on the super alloy GH4169, which is widely utilized in the aero-engine industry. They evaluated the hardness, microstructure, and tensile properties of the electron beam welded joints of GH4169. The high-temperature creep properties of these joints, with residual height, were also analyzed. Furthermore, the fatigue performance of the welded joints was tested, comparing those with and without residual height; the results indicated that the fatigue life of the joints without residual height was approximately ten times greater than that of those with residual height.

Beata Simekova et al. [28] performed an experiment on pure titanium Ti grade 2, 2 mm thick, which was welded to 2 mm thick nickel alloy 201 using electron beam welding. Various welding parameters were employed to create the butt-welded joints, with welding currents ranging from 40 to 70 mA and welding speeds of 20 to 50 mm/s. The study examined two beam offsets: one directed 100-300 µm towards the nickel side and the other 200 µm towards the titanium side. It was noted that the beam offset had a significant impact on the strength of the weld joints.

Georgi Kotlarski et al. [29] investigated the effects of different technological conditions of electron beam welding on the microstructure and mechanical properties of joints between the dissimilar alloys Ti6AI4V and AL6082-T6. In all experiments, the plates were preheated to 300°C. Various welding strategies were explored, including the ratio of electron beam current to welding speed, as well as applying a beam offset toward the aluminum side. The highest observed ultimate tensile strength was 165 MPa, accompanied by a yield strength of 80 MPa and an elongation figure of 18.4%.

Reisgen et al. [30] highlight that due to its high energy intensity and deep penetration capability, electron beam welding is particularly effective for welding steel plates with substantial wall thicknesses. Such plates are commonly utilized in offshore wind power systems. In their study, three different parameters with varying energy inputs were tested on three types of steel, using plates that had a wall thickness of 80 mm. The resulting top and bottom beads of the welds conformed to the DIN EN ISO 13919-1 standard. The parameters used resulted in an energy input per unit length ranging from 9.5 kJ/mm to 15.5 kJ/mm.

2. Selection of Materials

2.1 Metal Bases

Grades 2 and 5 of titanium (Ti-6Al-4V)

AISI 304 or 316L stainless steel

2.2 Materials for Fillers

Choose filler metals that help Ti and SS become more metallurgical compatible:

Ni-based filler, such as Inconel 625

Cu-based filler (Cu-Ni or pure Cu)

Tantalum or vanadium interlayers

Composites of Ti-SS graded alloys (if available)

3. Electron Beam Welding (EBW) is the welding process.

3.1 Setup of EBW Equipment

Make use of an EBW machine with a high vacuum chamber.

Level of chamber vacuum: less than 10⁻⁴ mbar

3.2 Process Elements to Be Improved

Current beam (mA)

voltage of beams (kV)

Speed of welding (mm/s)

Position of focus

(If used) Beam oscillation

Rate of filler feed (for external filler use)

Preheating (optional; controls the temperature gradient)

3.3 Design of Experiments

Make use of Response Surface Methodology (RSM) or Taguchi Design of Experiments (DoE):

Change the filler type, speed, voltage, and beam current.

Depending on the number of parameters, use a L9/L16 orthogonal array.

Three trials at the very least per configuration

4. Welding trials and sample preparation

4.1 Cooperative Design

Lap joint, butt joint, and dissimilar interface

Machining with strict tolerances

4.2 Welding Experiments

Use a variety of filler materials when welding.

Take note of any flaws in the welding (porosity, cracks, lack of fusion).

If the machine permits, use real-time monitoring.

4.3 Treatment After Welding

Weld cleaning and grinding

Post-weld heat treatment or controlled cooling are optional.

5. Testing and Characterization

5.1 Microstructural and Macrostructural Analysis

To investigate the fusion zone, use optical microscopy (OM).

Interface and microstructural characteristics of scanning electron microscopy (SEM)

Elemental analysis using energy dispersive X-ray spectroscopy (EDS)

Phase identification using X-Ray Diffraction (XRD) (intermetallics)

5.2 Examining Mechanically

Tensile testing is used to assess the strength of joints.

Microhardness mapping between the base metal, HAZ, and weld zone

Bend Testing: Weld ductility

Depending on the application, impact testing (Charpy) is optional.

5.3 Testing Without Damage (NDT)

Internal flaws in radiography and ultrasonic testing

Surface flaws detected by dye penetrant testing (DPT)

6. Analysis of Data

6.1 Analysis of Statistics

To identify important process parameters, use ANOVA (Analysis of Variance).

Create regression models for the following:

Tensile strength in relation to process variables

Hardness versus type of filler

6.2 Studies of Correlation

Link mechanical properties and microstructure.

Examine how intermetallic formation affects the strength of the weld.

6.3 Advanced/Optional Thermal Modeling

Utilize ANSYS or COMSOL software to perform thermal cycle finite element analysis (FEA).

Forecast the distribution of residual stress and intermetallic growth.

7. Verification and Replicability

To guarantee repeatability, repeat optimized trials at least three times.

Verify the optimized joints' metallurgical soundness and mechanical integrity.

8. Reporting and Documentation

Create thorough lab reports for every welding experiment.

Record pictures, charts, unprocessed data, and observations.

Write journal or conference publications based on:

A comparative analysis of filler materials

Failure analysis and interface microstructure

Optimizing EBW parameters for dissimilar welding

Bring in matplotlib.import pandas as pd import seaborn as sns import pyplot as plt

EBW trials sample experimental matrix experimental_matrix = pd.DataFrame({ 'Trial No.': [1, 2, 3, 4, 5, 6],

'Filler Material': ['Inconel 625', 'Cu', 'Ti-SS Alloy', 'Inconel 625', 'Cu', 'Ti-SS Alloy'],

'Beam Current (mA)': [40, 40, 40, 50, 50, 50],

"Welding Speed (mm/s)": [5, 5, 5, 7, 7, 7],

"Hardness (HV)": [220, 210, 235, 240, 215, 245];

"Tensile Strength (MPa)": [320, 300, 340, 360, 330, 370]

9.0 Tensile Strength Plot

plt.figure(figsize=(10, 5))

sns.barplot(data=experimental_matrix, x='Trial No.', y='Tensile Strength (MPa)', hue='Filler Material')

plt.title ("Tensile Strength of Welds with Different Filler Materials")

plt.ylabel('MPa Tensile Strength')

plt.xlabel('Trial Number')

plt.legend(title='Filler Material')

plt.grid (True)

plt.tight_layout()

plt.show()

Plot Hardness

plt.figure(figsize=(10, 5))

sns.lineplot(data=experimental_matrix, x='Trial No.', y='Hardness (HV)', marker='o', hue='Filler Material')

plt.title('Microhardness Across Welds')

plt.ylabel('Hardness (HV)')

plt.xlabel('Trial Number') plt.legend(title='Filler Material')

plt.grid(True), plt.tight_layout(), and plt.show()

Show the print of the experimental matrix ("Experimental Matrix for EBW Trials").

print(experimental_matrix)

methodology flow diagram

Material Selection

- Titanium (e.g., Ti-6Al-4V)

- Stainless Steel (e.g., 316L)

- Filler Materials (Ag, Cu, Nb, etc.)

Preparation

- Cutting and sizing of base metals

- Cleaning (e.g., acetone wash)

- Filler placement (foil/wire/sheets)

│

▼

Set- parameters:

• Beam current & voltage

• Focus & offset

• Weld speed

│  - Weld different filler setups

Post-Weld Characterization

- Visual inspection

- Non-destructive testing (NDT)

└────────┬────────────────────┘

Mechanical Testing

- Tensile strength

- Microhardness

- Elongation (%)

Microstructural Analysis

- Optical microscopy

- SEM/EDS                  │

- XRD (for intermetallics)

Results & Discussion

- Compare fillers

- Intermetallic formation

- Joint strength

│

Conclusion & Future Scope

- Best filler identified

- Suggestions for improvement

4.Result and Discussion:

Filler made of silver (Ag)

Interfacial intermetallics like Ti₂Ag were found in the weld joint in a study that used silver as the filler. Ti–Fe intermetallics were suppressed by all filler materials. Out of all the joints tested by Springer Link, the one with silver filler had the highest tensile strength, measuring about 310 MPa.

Filler made of copper (Cu)

With a tensile strength of roughly 310 MPa OSTI, copper was used as a filler to create a joint free of cracks caused by thermal stresses during cooling.

Another study demonstrated how copper's superior thermal conductivity resulted in improved mechanical properties, a refined microstructure, and a uniform temperature distribution. Among the compared filler materials, copper filler welds exhibited the highest elongation and improved residual stress profiles (MDPI).

### Niobium (Nb), Vanadium (V), Nickel (Ni), and Composite Fillers:

### Welds containing vanadium, nickel, and additional fillers showed various interfacial intermetallics (e.g., Fe₂Ti, Ni₃Ti, NiTi₂, etc.). The hardness and composition of those intermetallics were directly related to the range of tensile strengths. SpringerLink

### Micro-electron beam welding MDPI produced tensile strengths of up to 394 MPa in butt joint configurations with pure niobium as the filler.

### Joint compatibility was significantly improved by multilayer composite fillers, such as V/Cu composites, or multilayer stacks, such as Nb/Cu, Nb/Ni, and Ta/V/Fe. Using such combinations, one study demonstrated exceptional joint integrity (MDPIInfona) by achieving tensile strengths of up to 623 MPa, with failure occurring in the unmelted vanadium rather than the joint itself.

### 4.1 Summary Table

| Filler Material | Observations / Intermetallics | Tensile Strength (≈) | Additional Highlights |
| --- | --- | --- | --- |
| Silver (Ag) | TiAg intermetallics | ~310 MPa | Strongest among single fillers tested SpringerLink |
| Copper (Cu) | Cu–Ti intermetallics, refined microstructure | ~310 MPa | Crack-free welds, good elongation, uniform temp OSTIMDPI |
| Vanadium (V), Nickel (Ni) | Varied intermetallics (FeTi, NiTi, etc.) | Less than Cu/Ag | Properties tied to IMC hardness SpringerLink |
| Niobium (Nb) | Solid solution, no severe IMCs | up to ~394 MPa | Promising single-layer filler MDPI |
| Composite (e.g., V/Cu, Nb/Cu) | Multilayer fillers suppress IMCs | up to ~623 MPa | Failure outside joint, excellent performance MDPIInfona |

5. Conclusion:

Vanadium, nickel, and other filler-based welds showed various interfacial intermetallics (e.g., Fe₂Ti, Ni₃Ti, NiTi₂, etc.). Tensile strengths differed and were closely related to the comprehend current trends and developments, review recent research on machine learning applications in welding processes, paying particular attention to electron beam welding (EBW).  List the main conclusions of research that shows how machine learning affects the effectiveness and quality of welds.   Examine the approaches and results of several machine learning models that have been successfully applied to welding applications.

Examine recent studies on machine learning applications in welding processes, with an emphasis on electron beam welding (EBW), to understand current trends and advancements.  Enumerate the key findings of studies that demonstrate how machine learning impacts the quality and efficacy of welds.  Examine the methods and outcomes of a number of machine learning models that have been effectively used in welding applications. Examine the benefits of using machine learning in electron beam machining, taking cost-effectiveness, speed, and accuracy into account. 5. Examine case studies that illustrate the useful advantages of combining machine learning and electron beam welding in various sectors, such as the production of medical devices and aircraft.

Feature Scope

These results suggest a number of exciting avenues for additional study and improvement:

A. Multilayer Designs & Composite Interlayers

Superior tensile strengths (up to ~623 MPa) were attained by multilayer fillers, such as Nb/Cu, Nb/Ni, and Ta/V/Fe. To further lower IMCs and increase ductility, future research can investigate layer composition, thickness, and sequence optimization. MDPIInfona.

B. Biocompatible Options & Alternative Fillers

Further investigation of other β-stabilizing, biocompatible fillers (such as tantalum or niobium alloys) may result in high-performing joints with a broad range of applications, as niobium demonstrated strong potential in reaching over ~394 MPa tensile strength. The MDPI.

C. Process Control and Thermal Management

Because copper has a positive impact on residual stresses and thermal gradients, improved heat management techniques (such as thermal modeling, beam offsets, and cooling rates) may increase joint uniformity and reduce cracks. MDPI+1.

D. Customized Mitigation of Intermetallic

Better suppression of brittle phases may result from further investigation into the effects of beam parameters and filler chemistry on intermetallic formation. The promotion of ductile solid solutions over hazardous IMCs can be revealed by advanced characterization (SEM, XRD, EBSD, and nanoindentation) SpringerLink+1MDPI.

E. Studies Particular to Applications

Biocompatibility, corrosion resistance, and fatigue life must be carefully assessed for aerospace or medical-grade applications. Investigating Nb, Ta, or V-based combinations is crucial for implants because fillers like Cu/Ag are less preferred.

F. Sophisticated Testing Procedures

Future research should look at fatigue, fracture toughness, long-term durability, and corrosion testing in addition to tensile strength and microhardness, particularly for components that are essential to service.

G. Parameter optimization and modeling

The creation of optimal welding protocols may be sped up by combining design of experiments (DOE) for beam power, offset, and filler placement with computational models (such as phase diagrams and thermal stress simulations).

Concluding remarks

In conclusion, current research shows that titanium can be successfully electron beam welded to stainless steel using a range of filler materials. The most promising mechanical performance is offered by composite multilayer fillers, particularly copper, silver, and niobium. Future research should concentrate on improving these methods, comprehending intermetallic behavior, and guaranteeing their suitability for high-stress sectors like energy, aerospace, and medicine.

7. References:

- do not write  anythingnhere

- Muhammad ilyas, Tauheed shehbaz, Ghulam Hussain, and Mohammad Alkahtani, “Microstructural and mechanical characterization of electron beam welded low nickel nitrogen –strenthened austenitic stainless steel”, Heliyon, Vol.: 10, 2024, pp: e34315.

- Dutilleul.T, Widdison.R, and Kyffin, “Development of electron optical capabilities for manufacturing of large components by electron beam welding”, Welding in the World, vol: 68, 2024,  pp:  819-828.

- Min Cheng, Bingbing Yu, Ruipeng Guo, Xiaohui Shi, Lei  Xu, Junwei Qiao, and  Rui Yang, “Electron beam welding of a  novel near alpha high temperature titanium alloy powder compact: effect of post –welding heat treatment on tensile properties”, journal of material Research and technology,2021,10:153-163.

- Korad Kerber, Lars Halbauer, Horst Biemann, and Anja Buchwalder, “Suporession of spiking defects in deep penetration electron beam welding ETP copper” welding in the world, vol: 68, 2024, 1443-1459.

- Zbigniew Wencel, Sylwia Wiewiorowska, Pawel Wieczorek, Lacek Michalczyk, and Andrzej Gontarz, “Evaluation of the impact of electron beam welding parameters on the mechanical properties and microstructure of the resulting joint for 39CrMoV13 and M50NiL steel grades” Archives of civil and mechanical Engineering, 2022, 22:200.

- Bauer.A, Wiegand.M, Wicke.P, Sommer .N and vollmer.M, “electron beam welding of hot rolled Fe-Mn-Al-Ni shape memory alloy sheets”, Shap.Mem.superelasticity, Vol.: 9, 2023, pp: 364-376.

- Marta Lipinska, Florian Pixner, Ireneusz szachogluchowicz, Florian Mittermayr, Cyrill Grengg, Norbert Enzinger, and Malgorzata Lewandowska, “Application of electron beam welding technique for joining coarse-grained and ultrafine –grained plates from AL-Mg-Si-alloy”, Jounral of Manufacturing Processes, vol.: 104, 2024, pp: 28-43.

- VADIM S. TYNCHENKO, SERGEI O.KURASHKIN, VALERIA V. TYNCHENKO, VLADIMIR V. BUKHTOYAROV, VLADISLAV V.KUKARTSEV, ROMAN B. SERGIEKO, SERGEI V.TYNCHENKO, AND KIRILL A BASHMUR, “Software to predict the  process parameters of electron beam welding”, Digital  object identifier vol: 10.1109/ACCESS ,2021,3092221.

- Jia Tao ,  Jiefegng Wu  , Zhihong Liu, Jianguo Ma and Zhenfei Liu, “ A  New method for simulating  electron beam welding  process of niobium sheets with beam oscillation “ Mater.  Res .Express Vol.: 10, 2023, 016515.

- V.S.Tynchenko, I.A. Golovenok,  V.E.Petrenko, A.V.Milov, and A.V.Murygin, “ Gradient  boosting method application to  support process decision in the electron beam welding process “siberian journal of science  and technology .vol.: 21, 2020.

- Ariel Rokem and Kendrick Kay “Fractional ridge regression: a fast, interpretable reparameterization of ridge regression”, Giga.sciece vol.: 9, 2020, pp: 1-12.

- Vasundhara Singh, Gour  Gopal Roy, and prakash Srirangam, “Unveiling Impact of electron beam optics on weld attributes in EN30B steel “ Journal of optics and photonics research vol 1(3) ,2024,109-123.

- V.I.Zagorikov, V.M. Nesterenkov, Yu.V Orsa, and A.M. Ignatenko” Technologies of repairing cathode unit of electron beam gun with the use of electron beam welding “the’paton welding journal ,issue Vol.01, January 2023.

- Jozef Bata, Beata Simekova, Milan Maronek, and Maria Domankova “electron beam welding of 2099-T83 Aluminium –lithium alloy thick plates”, MATEC We of conferences Vol.: 269, 02010, 2019.

- M. Mohamed Jameel, Dr.B.Anandavel, R.Vinoth Babu, and D .Noorullah, “A literature Review on electron beam welding”, IJSART Vol.: 7 issue 9, Sep 2021.

- Oleksii Fedosov, and Olena Karpovych, “Determininig the technological parameters of electron beam welding of high strength titanium alloys”,

- R.Rai, T.V.Palmer, J.W.Elmer, and T.Debroy “Heat transfer and fluid flow during electron beam welding of  304L stainless steel alloy”

- A.A.Zenin, I.Y.Bakeev, A.S.Klimov, E.M.Oks, and A.V.Tyunkov, “The effect of temperature on electron beamb brazing of titanium to alumina ceramic”, supplement to the welding journal, February, 2023.

- V.M.Nesterenkov, K.S.Khripko and  V.A.Matiichuk “electron beam technologies of welding ,surfacing, prototyping : results and prospects “

- V.O.Shapovalov, V.G.Mogylateko, R.V.Lyutyi, and R.V.Kozin “ Nitrozen absorption by 04Cr18NI10 Steel in plasma-arc melting under slag of CaO-Al2O3 System “ the paton welding journal ,issue 01,January 2024.

- V.V.Skryabinsky, V.M.Nesterenkov, and M.O.Rusynykn, ” Impact of  heat treatment  on mechanical properties  of joints during electron beam welding of 2219 alloy” the  paton welding journal ,issue 01,January 2024.

- S.V.Akhonin, V.O.Beresos, O.G.Erokhin, O.O.Kotenko, M.I.Medvedev, and M.G.Lyashenko “Nickel scrap recycling by electron beam melting method”. The paton welding journal, issue 01, January 2024.

- Radoslav vandzura, matus gelatco, Michal hatala, Frantisek botko, and Svetlana radchenko, “Evaluation of electron beam welded joints properties of additively manufactured and conventional aluminium alloys”

- S.Yu. Maksymov, G.V.Fadeeva,  Jia Chuanbao,  V.A.Kostin, A.A Radzievskaya and , D.V.Vasilyev “Influence of cooling rate on microstructure and phase composition of HAZ of duplex (DSS) 2205 Steel in wet under water welding” The paton welding journal, issue, 01, January 2024.

- O.Ye.korotynskyi, M.P.Drachenko, A.M.Zhernosekov, and I.V.Vertetska, “Welding current formers using artificial long lines”, The paton welding journal, issue, 01, January 2024.

- Sihui Yang, Zhicheng Liu, Yong Zhang, and  Xiangyun Long, “the influence of electron beam welding technology on mechanical properties of GH4169 welded joints “

- Beata Simekova, Erika Hodulova, Pavel Kovcocy, Ingrid Kovarikova, Miroslav Sahul, Martin Sahul, Matej Pasak and Florian Pixner, “Influence of electron beam welding parameters on the microstructure formation and mechanical behaviors of the Ti and Ni dissimilar metals welded joints“

- Georgi Kotlarski, Darina Kaisheva, Maria Ormanova, Borislav Stoyanov, Vladimir Dunchev, Angle Anchev, and Stefan Valkov, “Improved join formation and ductility during electron beam welding of Ti6Al4V  and AI6082-T6 Dissimilar alloys“

- U.Reisgen, S.Olschok, and T.Evers, “Developmet of a robust welding process for electron beam welding of thick plates for construction offshore windturbines”